## Slide 1: Solving & Preventing Dimensional Accuracy Issues For the LPBF Process
Ryan Aday
07/25/2024 Divergence 3D Presentation

## Slide 2: Let’s get right into it…
MSME from Georgia Tech
Incoming MSEE from UC Boulder
PE, LSSBB
Designed & built 3D printers since middle school (FFF, SLA)
Raytheon
  Hands-on hardware, software, firmware fixes for Patriot
  Head/maintainer of FFF, SLS printers for prototype parts
Motor, servo controller experience w/ HyTech Racing

## Slide 3: LBPF Overview
Powder Deposition
Lasing
Solidification
Platform Realignment

## Slide 4: Dimensional Accuracy Issues
Material
Thermal Stress & Distortion
User-Based
Machine Calibration & Maintenance
Environmental Conditions
Design-Based
Powder Material Inconsistencies
Post-Processing Techniques
Support Structure Implementation
Laser Power Fluctuations
Build Plate Adhesion
Slicer Settings
Software, Firmware, Hardware (SFH) Limitations

## Slide 5: User-Based Issues
Machine Calibration & Maintenance
Issue: Servos, gyro, roller loses accurate movement/placement due to wear
Causes: Layer shifts, surface roughness, inaccuracies in the final dimensions
Environmental Conditions
Issue: Temperature, humidity, variations within the build chamber
Causes: Oxidation of the powder -> inconsistent melting
Post-Processing Techniques
Issue: Machining, stress-relieving, heat treatments induces additional stresses/removes material unevenly
Causes: Deviations from the desired dimensions and geometrical tolerances
Pre-Slice Techniques
Issue: The provided part slice/files are not properly resized to account for shrinkage
Causes: Undersized parts

## Slide 6: Material Issues
Thermal Stress & Distortion
Issue: Uneven cooling rates after lasing
Causes: Cracking, warpage
Powder Material Inconsistencies
Issue: Variations in powder particle size, shape, and distribution affect packing density, deposition
Causes: Variable melting behavior, voids
Build Plate Adhesion
Issue: Disadhesion between first layer & build plate
Causes: Layer shifts, misalignment of subsequent layers

## Slide 7: Design-Based Issues
Laser Power Fluctuations
Issue: Inconsistent laser power
Support Structure Implementation
Issue: Inadequate or excessive support structures
Slicer Settings
Issue: Non-ideal settings for chosen scan pattern, layer thickness, and laser speed
Causes: Residual stresses, anisotropic properties, and dimensional distortions
SFH Limitations
Causes: Uneven/inconsistent melting and solidification, increased solubility
Causes: Heat dissipation and/or part stability
Causes: Slicer resolution, beam diameter larger than required, servos inadequate for scan speeds, etc.
Issues: Fundamental with the design of the printer

## Slide 8: Root Cause Analysis Checklist
Immediate Checks
1. Were the scheduled maintenance/calibration intervals followed? (Gyros, bed-leveling, laser, servos, roller, powder depositor)
2. Was the print bed within permissible humidity & temperature range?
3. What post-processing techniques were used? (Machining, coating, heat treatments to spec)
4. Was the part sized properly to account for material shrinkage?
Deeper Dive (Material)
1. Are there any observed cracks in the print?
If yes, likely to be thermal stresses/distortion during cooling
2. Are voids present?
If yes, powder dimensionality or characteristics or lasing power out of spec
3. Observed layer lines?
If yes, poor bed adhesion/miscalibration.
Inherent Design Flaws/Stipulations
1. Is the laser emitting consistent power?
2. What, if any, support structures were used?
3. What were the slicer settings used to prepare the print?
And as a side note, are these the proper settings for the material/was the user modifying settings within acceptable ranges?
4. Surface artifacts? (scaling, pixelated surface, etc)
If yes, SFH issue possible.

## Slide 9: More Permanent Solutions
Eliminate variability from the user side
  Ensure powder consistency
    Sieve for dimensionality
      Vevor Sieve
      Can also check post-production using OpenCV to determine dimensional consistency for a sample
    X-ray Spectroscopy to determine powder purity & correct alloy mixture for redundancy
      Cheap sensor may be used to check before prints
      https://www.amptek.com/internal-products/x-123-complete-x-ray-spectrometer

## Slide 10: More Permanent Solutions (cont.)
  Built-in maintenance scheduler & provided checklist
    Both for slicing & setting up the printer
  Auto-calibration before prints
  Environmental & sensor data logger
    Temperature, humidity sensors to collect the past 1000 seconds and determine the moving average & variability
    Inkbird Hygrometer & Thermometer
    Voltage sensor for laser to determine energy output stability
      https://store.egauge.net/High-Voltage-Sensor

## Slide 11: More Permanent Solutions (cont.)
Continuous print checks
  OpenCV to identify cracks, voids, layer shifts, etc. during & after print
  If defect identified, stop print and issue recommendation
Develop optimized parameters for materials
  You need to optimize parameters to ensure print speed is as fast as possible while ensuring tolerances are in spec
    Feed rate
    Lasing power
    Hatch spacing
    Inherent powder dimensions and tolerances
    If applicable, isolate scan strategies, support structures permissible for material

## Slide 12: Implementation
My code:
  STL orienter & support structures
  Process control
  Powder dimensionality
  Parameter optimizer
  You can find my work here: https://github.com/ryan-aday/LBPF_Process_Optimizers

## Slide 13: How the Code Works: stl_orienter.py
Accepts user-provided STL
  STLs larger than 5000 KB will have quadratic edge collapse decimation for simplification
Orients the STL based on:
  Minimizing area per layer
  Reducing intersections of the model & base plate
  Note- L-BFGS-B chosen for speed and moderate accuracy for the STL file sizes typically encountered vs CG, SDG. Adam too slow as tested.
Provides the option to add “Cura-like” tree supports based on overhang angle (WIP)

## Slide 14: How the Code Works: process_control.py
Takes any CSV or JSON file format
  Assumes each column is a process parameter
  For each column, computes the mean & standard deviation
  UCL and LCL is the mean +/- 3*std
  Plots data points per column, with UCL & LCL
  If any points deviate from the UCL/LCL, process is out of control
    Suggests new targets based on the current mean

## Slide 15: How the Code Works: powder_hough.py
Uses OpenCV packages (also available in C++)
Binarizes image for easier edge detection
Gaussian blur to reduce noise
Canny edge detection to develop clearer distinction between edges
Hough Transforms to determine likelihood of circular features
  Minimum center distance, min & max radii, degree of probability, edge detection threshold (p1), accumulator threshold (p2)
Plots the recognized Hough circles atop provided image
May need to be tuned for larger images
  Fixed tunes if image capture standardized

## Slide 16: How the Code Works: param_opt.py
Uses:
  scipy minimization techniques
  Various material properties
Assumptions & Constraints:
  Constant laser beam diameter
  Targeted normalized enthalpy, solubility, shrinkage
Optimizes for minimum time to cool
Outputs the optimal laser power, scan speed, hatch spacing, layer thickness
Future improvements: characterize and constrain forces occurring during melt
  Research Link

## Slide 17: How the Code Works: param_opt.py Equations
Note: Uses references found in the repository.

## Slide 18: Questions?